## Slide 1: SpeedArc
Presented by Lorch
2012 | Lorch Schweißtechnik GmbH | www.lorch.eu
SpeedArc for more Speed!

## Slide 2
Contents:
Our innovation
Advantages and Use
Applications
Unit and Operation

## Slide 3: Our Innovation.

## Slide 4
Material transition at MIG/MAG welding
SpeedArc-range
ROTATING ARC
PULSE ARC
SHORT ARC
MIXED ARC
SPRAY ARC
VOLTAGE
MSG ARC RANGES ARE USING 1.2MM WIRE
WIRE SPEED
SpeedArc

## Slide 5: SpeedArc Penetration
power
voltage
travel speed
wire speed
a-Mass
e-Mass
total a-value
Speed-Arc
308A
30,4V
53cm/min
12m/min
5,5mm
2,8mm
8,3mm
Spray
312A
31,5V
40cm/min
10m/min
5,5mm
1,6mm
7,1mm

## Slide 6
Spray arc
Little Spatter whilst welding
Non-short-circuit droplet transmission
High energy density
Application at thick materials only
Deep penetration and wider seam geometry
High energy input per length and thus risk of distortion
Large heat affected zone

## Slide 7
SpeedArc
Is related to the spray arc range (high performance hybrid spray arc)
Significantly higher arc focusing
Higher energy density
Higher arc pressure in to the weldpool
Application from 3mm possible
Very little or no spatter

## Slide 8: SpeedArc penetration comparison
MIG/MAG-Standard
MIG/MAG-SpeedArc
smooth seam transitions
reduced heat affected zone
deeper penetration
Risk of undercut
normal penetration
larger heat affected zone

## Slide 9: Advantages/Use

## Slide 10: SpeedArc advantages/use
Deeper penetration due to high plasma pressure in the arc
Easy to use in manual welding applications due to incredibly stable arc
Less undercut
Increased profitability due to higher welding speed
Better seam quality in regard to the heat affected zone and less distortion due to less heat input
Minimal or no spatter formation

## Slide 11: SpeedArc effects/use
Root area is visibly better
Less seam preparation
Smaller weld prep angle required
  less material removal
  less filler material
  clear root capture
  according to requirements, thicker materials may be welded in a single pass
Smaller gaps, less layers, less gas, less filler materials
Longer stick-out possible

## Slide 12: SpeedArc effects/use
Can weld with a longer stick out
Obvious higher arc pressure
Easier placement of the arc into the root
Good toe/pool wettability
Torch angle less critical
More user friendly than standard Spray

## Slide 13
SpeedPulse
Referent:
2009 | Lorch Schweißtechnik GmbH | www.lorch.eu
Simply faster. Simply pulse.

## Slide 14: SpeedPulse
During the process the pulse remains
Unlike conventional pulse process 1 material continues to 2 flow between the Pulse 3
No short circuits
Has advantages on materials of 1 mm thickness and greater
For steel/stainless steel/aluminium

## Slide 15: SpeedPulse advantages

## Slide 16: SpeedPulse advantages

## Slide 17: 3-Steps to Weld Operating Concept
1. Operation mode 2- , 4-Stroke, Quatromatic
2. Wire/gas/material combination
(easy text dialogue)
3. Welding Curent

## Slide 18: SpeedArc/SpeedPulse advantages
Connection with long interpass hosepackages
Intermediate drive solutions
Digital PushPull-solutions

## Slide 19: Applications

## Slide 20: SpeedArc/SpeedPulse applications
Metal fabrication, plant and machinery construction
Vehicles, track-bound (rail) vehicles and shipbuilding
Container, device and equipment construction, offshore and others
Manual and mechanized /automated applications
mild steel
fine grained steel
stainless steel
aluminium

## Slide 21: SpeedArc/SpeedPulse applications
Metal construction, plant and machinery construction

## Slide 22: SpeedArc/SpeedPulse applications
Vehicles, track-bound (track) vehicles and shipbuilding

## Slide 23: SpeedArc/SpeedPulse applications
Container, device and equipment construction, offshore and others

## Slide 24: Thank you